THERMAL INSULATION

SECTION 07 21 19

Foamed-in-Place Insulation

SEALECTION 500

This specification utilizes the Construction Specifications Institute’s (CSI) 3-Part formatting.  The specification is a manufacturer-specific product specification to be used by design professionals as a guide specification.  Editing notes are indicated in red italics and precede specification text.  Delete editing notes in final specification.

This specification specifies medium density spray foam insulation by Huntsman Building Solutions.  Revise section number and title below to suit project requirements.

The specified product may contribute to the following credits/points for the respective rating system:

LEED V.4.1

National Green Building Standard (NGBS, ICC-700)

ERI (Energy Rating Index)

.

GENERAL

SECTION INCLUDES

** NOTE TO SPECIFIER **  Delete items below not required for project.

Spray-in-place semi-rigid open cell ½ pound polyurethane foam insulation in various assemblies, to provide an air barrier and improved thermal resistance.

RELATED SECTIONS

** NOTE TO SPECIFIER **  Delete any sections below not relevant to this project; add others as required.

Section 03 30 00 - Cast in Place Concrete.

Section 03 40 00 - Structural Pre-cast Concrete.

Section 04 20 00 - Unit Masonry.

Section 05 30 00 - Metal Decking.

Section 05 40 00 - Cold Formed Metal Framing.

Section 06 10 00 - Rough Carpentry.

Section 07 10 00 - Waterproofing.

Section 07 26 00 - Vapor Barrier.

Section 07 40 00 - Preformed Roofing and Cladding/Siding.

Section 07 65 00 - Flexible Flashing.

Section 07 80 00 – Fire protection.

Section 07 81 00 – Applied Fireproofing.

Section 09 20 00 - Gypsum Board.

Section 09 22 00 - Metal Support Systems.

REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

American Society for Testing and Materials (ASTM):

ASTM C 423 - Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

ASTM C 518 - Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

ASTM E 96 - Standard Test Methods for Water Vapor Transmission of Materials.

ASTM E 283 - Standard Test Method for Determining Rate of Air Leakage Through Exterior Windows, Curtain Walls, and Doors Under Specified Pressure Differences Across the Specimen.

ASTM E 2178: Standard Test Method for Air Permeance of Building Materials

ASTM E 413 - Classification for Rating Sound Insulation.

ASTM D 1622 Standard Test Method for Apparent Density of Rigid Cellular Plastics

ASTM E 119 Standard Test Methods for Fire Tests of Building Construction and Materials

ASTM E 970 Standard Test Method for Critical Radiant Flux of Exposed Attic Floor Insulation Using a Radiant Heat Energy Source

CAN/ULC S774-09 Standard Laboratory Guide for the Determination of Volatile Organic Compound Emissions from Polyurethane Foam

ASTM D 1621 Standard Test Method for Compressive Properties of Rigid Cellular Plastics

ASTM D 1623 Standard Test Method for Tensile and Tensile Adhesion Properties of Rigid Cellular Plastics

ASTM D 1929 Standard Test Method for Determining Ignition Temperature of Plastics

National Fire Protection Association (NFPA):

NFPA 286 Standard Methods of Fire Tests for Evaluating Contribution of Wall and Ceiling Interior Finish to Room Fire Growth

NFPA 285 Standard Fire Test Method for Evaluation of Fire Propagation Characteristics of Exterior Wall Assemblies Containing Combustible Components

International Code Council – International Residential Code:

Section 103.7 - Alternate Materials and Methods.

2012, 2015, 2018, 2021 IRC Section R314 - Foam Plastic Insulation.

2012, 2015, 2018, 2021 IRC Section R316 - Foam Plastic Insulation.

Section 806.4 – Unvented Attic Assemblies.

International Code Council – International Building Code:

Section 104.11 Alternative materials, design and methods of construction and equipment.

Section 2603 Foam Plastic Insulation.

SUBMITTALS

Submit under provisions of Section 01300.

Before commencing work, submit in accordance with local code.

Submit technical data sheets and samples as required by local code officials.

Submit the technical data sheet from the manufacturer showing the test results from the ASTM E84 (Surface Burning Characteristics).

Product Data: Manufacturer's data sheets on each product to be used, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

QUALITY ASSURANCE

Installer Qualifications:

Contractor performing work under this section shall be authorized by HUNTSMAN BUILDING SOLUTIONS in the art of applying spray polyurethane foam insulation.

Provide current HUNTSMAN BUILDING SOLUTIONS Authorized Contractor Certificate.

** NOTE TO SPECIFIER ** Include a mock-up if the project size and/or quality warrant taking such a precaution.  The following is one example of how a mock-up on a large project might be specified.  When deciding on the extent of the mock-up, consider all the major different types of work on the project.

Mock-Up:  Provide a mock-up for evaluation of surface preparation techniques and application workmanship.

Finish areas designated by Architect.

Do not proceed with remaining work until installation is approved by Architect.

Rework mock-up area as required to produce acceptable work.

DELIVERY, STORAGE, AND HANDLING

Materials shall be delivered in manufacturer’s original containers clearly labelled with manufacturer’s name, product identification, safety information, net weight of contents and expiration date.

Material shall be stored in a safe manner and where the temperatures are in the limits specified by the material manufacturer.

Empty containers shall be removed from site on a daily basis.

Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.

PROJECT CONDITIONS

Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

Ventilate insulation application area in accordance with the Spray Foam Coalition’s Guidance on best practices for the installation of Spray Polyurethane Foam.

Protect workers as recommended by the Spray Foam Coalition’s Guidance on best practices for the installation of Spray Polyurethane Foam.

Protect adjacent surfaces, windows, equipment and site areas from damage of overspray.

WARRANTY

Manufacturer’s Warranty:  HUNTSMAN BUILDING SOLUTIONS warrants spray-in-place urethane foam insulation, when installed by certified contractors using factory-trained applicators and applied in accordance with the Installation Instructions, will perform as stated in the Product Technical Data Sheet.

This warranty is in effect throughout the life of the building provided the original purchaser registers with the Warranty Department of the Manufacturer within thirty days of occupancy.

Manufacturer’s sole responsibility under this Limited Lifetime Warranty shall be to repair or replace any defective Product at the cost of the material only.

Manufacturer shall not be responsible for labor cost or any other costs whatsoever related to, or in connection with the removal or installation of either the original or replacement product.

Refer to www.huntsmanbuildingsolutions.com for full warranty terms.

PRODUCTS

  - ENVIRONNEMENTAL REQUIREMENTS

    - The product shall have a generic industry Environmental Product Declaration (EPD).

MANUFACTURERS

    - Acceptable Manufacturer:  HUNTSMAN BUILDING SOLUTIONS

3315 East Division Street, Arlington, TX 76011.

(855) 942-7273.

architect@huntsmanbuilds.com

http://www.huntsmanbuildingsolutions.com

** NOTE TO SPECIFIER ** Delete two of the following three paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Equivalent as judged by Architect

      - Contact HUNTSMAN BUILDING SOLUTIONS Building Science and Engineering Department for product comparison data

        - 855-942-7273

        - architect@huntsmanbuilds.com

SPRAY FOAM INSULATION

** NOTE TO SPECIFIER **. Delete if not required.

Spray Applied Semi Rigid Polyurethane Foam Insulation System: Open Cell ½ pound Foam Product: SEALECTION® 500

Manufactured by HUNTSMAN BUILDING SOLUTIONS, Arlington, TX.

Product Approval:

International Code Council Evaluation Services Report #1172.

Approved for building types I, II, III, IV, & V

Passed NFPA 286 in accordance with IBC 803.2.

CCMC Evaluation # 12697-R..

Installation:

Application with a prescriptive Thermal Barrier:

Up to 9-1/4 inches (235 mm) for wall cavities and 14 inches (356mm) in floors or ceilings with 1/2 inch gypsum wall board or equivalent 15 minute thermal barrier in accordance with IBC 2603.4 or IRC R316.4.

Application without a Thermal or Ignition Barrier (exposed foam)

Up to 7-1/2 inches (191mm) in walls and 11 ½  inches (292mm) in floors and ceilings with all foam surfaces covered with 9 dry mils (0.23mm) [14 wet mils (0.356mm)] of DC315.

Application without a Thermal or Ignition Barrier (exposed foam)

Up to 7-1/2 Inches (191 mm) in walls and 11-1/2 inches (292 mm) in floors and ceilings with all foam surfaces covered with 11 dry mils (.28 mm) [ 17 wet mils (.43 mm)] of BLAZELOKTM TBX.

Attics and Crawlspaces: Passed AC 377 Appendix X compliant NFPA 286.

Application with Blazelok™ IB4 Intumescent Coating:

Up to 9-1/2 inches (241mm) on vertical surfaces and 11-1/2 inches (292mm) on the underside of the top of the space with all foam surfaces covered with a minimum nominal thickness of 5 dry mils (0.13mm) [9 wet mils (0.23mm)] of Blazelok™ IB4.

Application with Andek Fireguard Intumescent Coating:

Up to 9-1/2 inches (241mm) on vertical surfaces and 11-1/2 inches (292mm) on the underside of the top of the space with all foam surfaces covered with a minimum nominal thickness of 10 dry mils (0.25mm) [20 wet mils (0.51mm)] of Andek Fireguard.

Application with No-Burn® Plus XD Intumescent Coating

Up to 9-1/2 inches (241mm) on vertical surfaces and 11-1/2 inches (292mm) on the underside of the top of the space with all foam surfaces covered with a minimum nominal thickness of 6 dry mils (0.15mm) [10 wet mils (0.25mm)] of No-Burn® Plus XD.

Use on Attic Floors:

Up to 9-1/2 inches (241mm) between and over the joists in an attic floor.  All foam surfaces must be covered by one of the following intumescent coatings:

Blazelok™ IB4: 5 dry mils (0.13mm) [9 wet mils (0.23mm)]

Andek Fireguard: 10 dry mils (0.25mm) [20 wet mils (0.51mm)]

No-Burn® Plus XD: 6 dry mils (0.15mm) [10 wet mils (0.25mm)]

One-Hour Fire-Resistance-Rated Wall Assemblies: Non load-bearing

Refer to ESR1172 Section 4.5

Exterior Walls of Type I, II, III, and IV

Up to 3-5/8 inches (92mm)

Non load-bearing NFPA 285-tested Wall Assembly

Refer to ESR 1172 Section 4.6.1

Physical Properties:

| Density | ASTM D1622 | 0.45 - 0.5 lb/ft³ | 7.2 - 8 Kg/m³ |
| --- | --- | --- | --- |
| Thermal Resistance | ASTMC518, at 1’’ | R-3.81 | 0,67 |
| Compressive strength | ASTM D1621 | 0.7 psi | 4.8 KPa |
| Tensile strength | ASTM D1623 | 5.6 psi | 38.6 KPa |
| Air Permeance | ASTM E 283 3.5’’ @ 75 Pa | 0.001 L/s· m² |
| Air Permeance | ASTM E 2178-13 3.5’’ @ 50 Pa 3.5’’ @ 100 Pa 3.5’’ @ 300 Pa | 0.001 L/s· m² 0.003 L/s· m² 0.008 L/s· m² |
| VOC | CAN/ULC S774 | 1 day |
| Spontaneous Ignition Temperature | ASTM D1929 | 560oC | 1040oF |
| Water vapour permeance | ASTM E96 3.5’’ 5.5’’ 7’’ 10’’ | 6.33 perms 4.03 perms 3.17 perms 2.20 perms | 362 ng/Pa s.m² 231 ng/Pa s.m² 181 ng/Pa s.m² 126 ng/Pa s.m² |
| Noise Reduction Coefficient (NRC) | ASTM C423 | 0.75 |
| Sound Transmission Class (STC) | ASTM E413 | 49 - 51 |
| Surface Burning Characteristics | ASTM E84 | Class 1 |
| Flame Spread Index | ASTM E84 | 21 |
| Smoke Development | ASTM E84 | 216 |
| Commercial Fire Resistance | ASTM E 119 | 1 hour load bearing |
| Commercial Fire Resistance | NFPA 285 | Assembly Passed |
| Attic Floor Uncoated Thickness | ASTM 970 | 14’’ |

- Equipment used to apply the foam insulation shall have fixed ratio positive

displacement pumps and approved by foam manufacturer.

Equipment used to apply the Water Based intumescing coating shall be an airless sprayer    approved by the manufacturer.

ACCESSORY PRODUCTS

A. 	Water Based intumescing coating:

Product: BLAZELOK™ IB4, Distributed by HUNTSMAN BUILDING SOLUTIONS, Manufactured by ICP Group.

Product: BLAZELOK™ TBX, Distributed by HUNTSMAN BUILDING SOLUTIONS, Manufactured by ICP Group.

DC 315 Distributed by HUNTSMAN BUILDING SOLUTIONS, Manufactured by International Fireproof Technology Inc.

Product: No-Burn® plus XD, Manufactured by No-Burn Inc.

Product: Andek Fireguard, manufactured by Andek Corporation.

Primers:

Product: Adbond manufactured by Adfast or Thermo-Prime by HUNTSMAN

BUILDING SOLUTIONS

Application: Follow manufacturer’s application recommendations.

Recommended for oily surfaces and galvanized steel like Z-bar, PVC, curtain walls and steel decks

EXECUTION

EXAMINATION

Do not begin installation until substrates have been properly prepared.

If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

Commencement of work outlined in this section shall be deemed as acceptance of existing work and conditions.

PREPARATION

Clean surfaces thoroughly prior to installation.

Apply only when surfaces and environmental conditions are within limits prescribed by the material manufacturer.

Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

It is recommended to install primer on oily surfaces and galvanized steel

INSTALLATION

Install in accordance with manufacturer's instructions.

Apply as recommended by manufacturer to thickness as indicated on drawings.

Equipment used to apply the foam insulation shall have fixed ratio positive

displacement pumps approved by foam manufacturer.

PROTECTION

Protect installed products until completion of project.

Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION 07 21 19